TECHNICAL DATA SHEET

RTV-2 Platinum Cure Silicone Rubber

Shore A 70

Product Description

RTV-2 Platinum Cure Silicone Rubber 70A is a two-component addition-cure silicone elastomer designed for room-temperature or heat-accelerated curing. The cured rubber exhibits excellent dimensional stability, low shrinkage, good elasticity, and outstanding resistance to heat, aging, and weathering.

It is suitable for industrial molds, rollers, pads, seals, cushioning components, and other applications requiring high hardness silicone rubber.

This product is also suitable for protecting sensitive electronic components and industrial assemblies requiring a relatively rigid yet resilient silicone encapsulant.

Typical Properties (Uncured)

| Property | Unit | Value |
| --- | --- | --- |
| Appearance | - | Translucent Liquid |
| Mixing Ratio (A:B) | - | 1:1 |
| Pot Life (25°C) | min | 30 |
| Cure Time (25°C) | hrs | 4 |
| Specific Gravity | g/cm³ | 1.12 |

Typical Properties (Cured)

Tested after complete curing at 25°C.

| Property | Unit | Value |
| --- | --- | --- |
| Hardness | Shore A | 67 |
| Tensile Strength | MPa | 3.4 |
| Elongation at Break | % | 220 |
| Tear Strength | kN/m | 6.5 |
| Linear Shrinkage | % | <0.1 |

Features

- Platinum-catalyzed addition cure system

- Room temperature curing

- Low shrinkage

- Good dimensional stability

- Excellent aging resistance

- Excellent heat resistance

- Non-toxic and odorless after curing

Typical Applications

- Industrial molds

- Silicone rollers

- Cushioning pads

- Electronic components

- General industrial silicone products

Storage and Shelf Life

Store in the original unopened containers in a cool and dry place at temperatures between 5°C and 30°C.

Shelf Life: 12 months from the date of manufacture.

Packaging

- Part A: 20 kg/drum

- Part B: 20 kg/drum

Other package sizes are available upon request.

Disclaimer

The information contained herein is based on laboratory testing and practical experience. The values shown are typical properties and should not be used for preparing specifications. Users should evaluate the suitability of the product for their specific application.