TECHNICAL DATA SHEET
RTV-2 Platinum Cure Silicone Rubber
Shore A 70
Product Description
RTV-2 Platinum Cure Silicone Rubber 70A is a two-component addition-cure silicone elastomer designed for room-temperature or heat-accelerated curing. The cured rubber exhibits excellent dimensional stability, low shrinkage, good elasticity, and outstanding resistance to heat, aging, and weathering.
It is suitable for industrial molds, rollers, pads, seals, cushioning components, and other applications requiring high hardness silicone rubber. 
This product is also suitable for protecting sensitive electronic components and industrial assemblies requiring a relatively rigid yet resilient silicone encapsulant.

Typical Properties (Uncured)
	Property
	Unit
	Value

	Appearance
	-
	Translucent Liquid

	Mixing Ratio (A:B)
	-
	1:1

	Pot Life (25°C)
	min
	30

	Cure Time (25°C)
	hrs
	4

	Specific Gravity
	g/cm³
	1.12



Typical Properties (Cured)
Tested after complete curing at 25°C.
	Property
	Unit
	Value

	Hardness
	Shore A
	67

	Tensile Strength
	MPa
	3.4

	Elongation at Break
	%
	220

	Tear Strength
	kN/m
	6.5

	Linear Shrinkage
	%
	<0.1



Features
· Platinum-catalyzed addition cure system
· Room temperature curing
· Low shrinkage
· Good dimensional stability
· Excellent aging resistance
· Excellent heat resistance
· Non-toxic and odorless after curing

Typical Applications
· Industrial molds
· Silicone rollers
· Cushioning pads
· Electronic components
· General industrial silicone products

Storage and Shelf Life
Store in the original unopened containers in a cool and dry place at temperatures between 5°C and 30°C.
Shelf Life: 12 months from the date of manufacture.

Packaging
· Part A: 20 kg/drum
· Part B: 20 kg/drum
Other package sizes are available upon request.

Disclaimer
The information contained herein is based on laboratory testing and practical experience. The values shown are typical properties and should not be used for preparing specifications. Users should evaluate the suitability of the product for their specific application.

